Supplementary Material (ESI) for Chemical Communications

This journal is © The Royal Society of Chemistry 2002

Typical procedure for synthesis of 1: A mixture of NH4VO3 (3.0 mmol), H3[P(Mo3O10)4]× xH2O (0.5 mmol), Co(en)3Cl3(1.0 mmol), 2,2’-bipyridine(1.0mmol) and H2O(18ml) was stirred over 20 min, and then transferred into a 25ml Teflon-lined steel autoclave. The mixture was heated at 170 °C for 6 days, 530 mg dark block crystals of 1 were separated from the blue mother solution. IR (KBr pellet, cm-1): 3435(b, s), 3217(b,s), 3082(m), 1599(m), 1566(w), 1473(w), 1443(m), 1315(w), 1249(w), 1160(w), 1056(w), 1023(w), 951(vs), 769(s), 712(s), 651(m). XPS (eV): Co2p3 /2(781.3), V2p3/2 (516.5) and Mo3d5/2 (231.9).