Supplementary Material (ESI) for Chemical Communications

This journal is © The Royal Society of Chemistry 2002

Dimeric Iron N-Confused Porphyrin

Contents

General information

Preparation of  [Fe(NCTPP)]2 (6)

Preparation of [Fe(ONCTPP)]2(OH)•Na(THF)2 (7)

Absorption spectra of [FeII(NCTPP)]2 (6) and [Fe(NCOTPP)]2(OH)•Na(THF)2 (7) (Supporting Figure 1)

SQUID magnetic susceptibility data for [Fe(NCTPP)]2 (6) (Supporting Figure 2)

SQUID magnetic susceptibility data for [Fe(NCOTPP)]2(OH)•Na(THF)2 (7) (Supporting Figure 3)

Crystal structure report for 6

Crystal structure report for 7

___________________________________________________________________________

General Information

Manipulations, reactions and transfers of samples were conducted under nitrogen in an inert atmosphere dry box or according to standard Schlenk techniques.  For inert-atmosphere operation, solvents were dried, distilled, and degassed using standard techniques.  Pyrrole was fresh distilled from calcium hydride before use. Otherwise all starting materials were obtained commercially and used without further purification. UV-Vis spectra were recorded on a Hewlett Packard 8453 spectrophotometer.  Analysis of carbon, hydrogen and nitrogen were obtained with a CHN analyzer (Heraeus).  Magnetic susceptibility data were recorded on a Quantum Design MPMS5 5 T SQUID magnetometer.  The SQUID results were obtained with a field of 10000 G.

Preparation of [Fe(NCTPP)]2 (6).  A 50 mL vessel charged with a THF (20 mL) solution of Fe(NCTPP)Br (50 mg, 0.067 mmol) was added with NaSePh (15 mg, 0.084 mmol) in an inner atmosphere dry box.  The solution was heated to 60° C and continuously stirred under nitrogen.  After 6 h, the solution was cool down to room temperature and the solution was concentrated to about 5 ml under vacuum.  The excess NaSePh and any precipitated salt were removed by filter the solution through celite.  After dry the solution under vacuum, the solid was redissolved in 10 mL of CH2Cl2 and filter through celite.  The solution was dried under vacuum and redissolved in 5:1 of THF/CH2Cl2 and diffused with n-hexane.  Chunky dark green solid crystallized out from the solution  and the solid was collected and washed with hexane to have 76 mg of [Fe(NCTPP)]2. (85.2 %) A crystal suit for X-ray crystal analysis was picked directly from the vial and seal with epoxy glue immediately. [Fe(NCTPP)]2: Absorption spectrum (CH2Cl2) [max, nm (log , M-1 cm-1)]: 459(4.62), 755(3.93).  Anal. Calcd for Fe2C44H56N8 •2THF•1.5CH2Cl2: N, 6.96; C, 72.79; H, 4.69. Found: N, 6.82; C, 72.88; H, 4.56.

Preparation of [Fe(ONCTPP)]2(OH)•Na(THF)2 (7).  In a 50 ml flask charged with 20 mL THF was added with Fe(NCTPP)Br (50 mg, 0.067 mmol) and NaSePh (60 mg, 0.335 mmol) in an inert atmosphere dry box.  The solution was stirred at 60° in dry box and cooling to room temperature after 24 h. A UV-vis spectrum of λmax at 455 nm with pattern similar to 6 was observed.  The reaction flask was then taken out from dry box and exposed to air for about 1 min with stirring at room temperature.  The λmax of UV-vis shifted rapidly from 455 to 389 nm within 5 min. The solution was stirred continuously for another hour.  The solvent was then removed under vacuum and the yellow-brownish solid was sent into box and dissolved in 15 mL of 5:1 THF/CH2Cl2.  The solution was filtered through celite, concentrated to about 5 ml and layer with n-hexane.  Crystals formed after several days were collected and washed with hexane to have 74 mg of [Fe(ONCTPP)]2(OH)•Na(THF)2. (72 % yield)  [Fe(NCOTPP)]2(OH)•Na(THF)2: Absorption spectrum (CH2Cl2) [max, nm (log , M-1 cm-1)]: 389(4.83).  Anal. Calcd for  Fe2O5C96N8H71Na1•2CH2Cl2: N, 6.51; C, 68.39; H, 4.39. Found: N, 6.46; C, 68.57; H, 4.03.

X-ray Analysis of the Structures of 6 and 7

Diffraction measurements were carried out at 295(2) K on a Bruker SMART 1000 CCD diffractometer with graphite-monochromated Mo K radiation ( = 0.7107 Å).  Least-squares refinement of the positional and anisotropic thermal parameters for the contribution of all non-hydrogen atoms and fixed hydrogen atoms was based on F2. A SADABS absorption correction was made.  The SHELXTL structural refinement program was employed.

6: The crystal suits for structure analysis measured 0.36 x 0.27 x 0.08 mm3 which was grown from a slow diffusion of hexane into the THF/CH2Cl2 solution of 6 in an inert-atmosphere anaerobic dry box.  6 crystallized in monoclinic unit cell, space group Pbca, a =15.867(5) Å, b = 20.697 (6) Å, c = 22.397(7) Å,=90,  =90, =90 V = 7355(4) Å 3, Z = 4, Dc = 1.338 Mg/m-3,   = 0.71073 Å, = 0.454 mm-1, F(000) = 3088.  Data were collected for 1.82 <  < 27.67.  The structure was solved by direct method and refined by least square against F2 to R1 = 0.0756 (wR2 = 0.1546) and Sgoof = 0.983.

7: The crystal suits for structure analysis measured 0.38 x 0.14 x 0.10 mm3 which was grown from a slow diffusion of hexane into the THF/CH2Cl2 solution of 7 in an inert-atmosphere anaerobic dry box.  7 crystallized in monoclinic unit cell, space group C2/c, a = 28.473(3) Å, b = 18.7702(18) Å, c = 16.8963(16) Å,= 90, = 104.922(2), = 90 , V = 8725.6(14) Å 3, Z = 4, Dc = 1.346 Mg/m-3,   = 0.71073 Å, = 0.404 mm-1, F(000) = 3704.  Data were collected for 1.31 <  < 25.02.  The structure was solved by direct method and refined by least square against F2 to R1 = 0.0702 (wR2 = 0.1815) and Sgoof = 0.924.

Supporting Figure 1. Absorption spectrum for [Fe(NCTPP)]2 (6) (solid line) and [Fe(ONCTPP)]2(OH)•Na(THF)2 (7)(dotted line)

Supporting Figure 2. SQUID magnetic susceptibility data for  [Fe(NCTPP)]2 (6)

Supporting Figure 3. SQUID magnetic susceptibility data for [Fe(NCOTPP)]2(OH)•Na(THF)2 (7).

Crystal Structure Report for [Fe(NCTPP)]2 (6)

Table 1.  Crystal data and structure refinement.

Table 2.  	Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103).

Table 3.   Bond lengths [Å] and angles [°].

Table 4.   Anisotropic displacement parameters  (Å2x 103)

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

Supporting Figure 5. Views of [Fe(NCTPP)]2 (6) with atomic labelling Scheme.  Thermal ellipsoids are scales to 35% probability level.

Table 1.  Crystal data and structure refinement for h200m.

Identification code 	h200m

Empirical formula 	C96 H72 Fe2 N8 O2

Formula weight 	1481.32

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pbca

Unit cell dimensions	a = 15.867(5) Å	= 90°.

b = 20.697(6) Å	= 90°.

c = 22.397(7) Å	 = 90°.

Volume	7355(4) Å3

Z	4

Density (calculated)	1.338 Mg/m3

Absorption coefficient	0.454 mm-1

F(000)	3088

Crystal size	0.36 x 0.27 x 0.08 mm3

Theta range for data collection	1.82 to 27.67°.

Index ranges	-15<=h<=20, -23<=k<=26, -29<=l<=29

Reflections collected	45278

Independent reflections	8528 [R(int) = 0.1119]

Completeness to theta = 27.67°	99.3 %

Absorption correction	Empirical Used SADABS

Max. and min. transmission	0.9486 and 0.7211

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	8528 / 0 / 462

Goodness-of-fit on F2	0.983

Final R indices [I>2sigma(I)]	R1 = 0.0756, wR2 = 0.1546

R indices (all data)	R1 = 0.2719, wR2 = 0.1788

Largest diff. peak and hole	0.782 and -0.651 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103)

for h200m.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Fe(1)	9519(1)	236(1)	6042(1)	73(1)

N(1)	9811(3)	-551(2)	6603(2)	61(1)

N(2)	9283(3)	766(2)	6780(2)	60(1)

N(3)	8538(3)	742(2)	5620(2)	63(1)

N(4)	9504(3)	-665(2)	4465(2)	53(1)

C(1)	9958(4)	-1200(3)	6473(3)	64(2)

C(2)	10255(4)	-1526(3)	6996(3)	80(2)

C(3)	10322(4)	-1086(3)	7429(3)	77(2)

C(4)	10038(4)	-477(3)	7189(3)	64(2)

C(5)	10010(4)	105(3)	7527(3)	66(2)

C(6)	9646(4)	681(3)	7330(3)	67(2)

C(7)	9521(4)	1243(3)	7687(3)	75(2)

C(8)	9066(4)	1661(3)	7375(3)	76(2)

C(9)	8899(4)	1361(3)	6805(3)	65(2)

C(10)	8395(4)	1617(3)	6359(3)	65(2)

C(11)	8196(4)	1317(3)	5820(3)	66(2)

C(12)	7616(4)	1563(3)	5394(3)	79(2)

C(13)	7614(4)	1147(3)	4931(3)	72(2)

C(14)	8180(4)	642(3)	5052(3)	60(2)

C(15)	8420(4)	147(3)	4663(3)	58(2)

C(16)	8947(4)	-363(3)	4863(3)	61(2)

C(17)	8991(4)	-598(3)	5445(3)	61(2)

C(18)	9527(4)	-1129(3)	5439(3)	55(2)

C(19)	9790(4)	-1163(3)	4839(3)	80(2)

C(20)	9858(4)	-1488(3)	5923(3)	63(2)

C(21)	8012(5)	2275(4)	6456(4)	81(2)

C(22)	7379(7)	2363(5)	6829(4)	142(4)

C(23)	7026(9)	2967(7)	6905(5)	184(6)

C(24)	7309(9)	3466(6)	6633(5)	154(6)

C(25)	7946(7)	3416(5)	6224(5)	155(4)

C(26)	8304(5)	2806(5)	6153(4)	138(3)

C(27)	8079(4)	131(3)	4043(3)	66(2)

C(28)	8056(4)	654(3)	3673(3)	78(2)

C(29)	7694(5)	588(4)	3110(3)	101(3)

C(30)	7371(5)	29(5)	2928(4)	111(3)

C(31)	7400(5)	-498(4)	3291(4)	130(3)

C(32)	7760(5)	-445(4)	3842(3)	101(2)

C(33)	10111(5)	-2167(3)	5810(3)	68(2)

C(34)	9574(6)	-2605(4)	5625(4)	147(4)

C(35)	9790(6)	-3245(4)	5515(5)	158(4)

C(36)	10559(7)	-3449(4)	5576(4)	107(3)

C(37)	11131(6)	-3024(4)	5732(4)	154(4)

C(38)	10894(6)	-2385(4)	5858(4)	139(4)

C(39)	10333(5)	73(3)	8146(3)	72(2)

C(40)	11126(5)	310(3)	8263(3)	94(2)

C(41)	11452(6)	258(4)	8836(4)	117(3)

C(42)	10988(8)	-8(4)	9274(4)	125(4)

C(43)	10207(6)	-237(4)	9167(4)	117(3)

C(44)	9892(5)	-197(3)	8594(3)	94(2)

O(1)	1146(10)	2025(6)	6651(5)	376(6)

C(45)	564(9)	2575(7)	6489(6)	290(7)

C(46)	1095(10)	3063(7)	6241(7)	290(7)

C(47)	1669(12)	2659(9)	5999(7)	344(9)

C(48)	1907(12)	2313(8)	6431(8)	355(10)

________________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [°] for  h200m.

_____________________________________________________

Fe(1)-N(2) 	2.017(5)

Fe(1)-N(3) 	2.101(5)

Fe(1)-N(1) 	2.110(4)

Fe(1)-N(4)#1 	2.117(5)

Fe(1)-C(17) 	2.341(5)

N(1)-C(4) 	1.370(6)

N(1)-C(1) 	1.394(6)

N(2)-C(6) 	1.372(6)

N(2)-C(9) 	1.376(6)

N(3)-C(11) 	1.380(6)

N(3)-C(14) 	1.410(6)

N(4)-C(19) 	1.404(7)

N(4)-C(16) 	1.403(6)

N(4)-Fe(1)#1 	2.117(5)

C(1)-C(20) 	1.377(7)

C(1)-C(2) 	1.432(7)

C(2)-C(3) 	1.335(7)

C(3)-C(4) 	1.442(7)

C(4)-C(5) 	1.424(7)

C(5)-C(6) 	1.396(7)

C(5)-C(39) 	1.482(8)

C(6)-C(7) 	1.424(7)

C(7)-C(8) 	1.326(7)

C(8)-C(9) 	1.443(7)

C(9)-C(10) 	1.386(7)

C(10)-C(11) 	1.394(7)

C(10)-C(21) 	1.506(8)

C(11)-C(12) 	1.420(7)

C(12)-C(13) 	1.347(7)

C(13)-C(14) 	1.405(7)

C(14)-C(15) 	1.397(7)

C(15)-C(16) 	1.420(7)

C(15)-C(27) 	1.490(7)

C(16)-C(17) 	1.393(7)

C(17)-C(18) 	1.390(7)

C(18)-C(19) 	1.409(7)

C(18)-C(20) 	1.415(7)

C(20)-C(33) 	1.483(8)

C(21)-C(22) 	1.319(9)

C(21)-C(26) 	1.372(9)

C(22)-C(23) 	1.381(11)

C(23)-C(24) 	1.282(13)

C(24)-C(25) 	1.367(13)

C(25)-C(26) 	1.393(10)

C(27)-C(28) 	1.365(7)

C(27)-C(32) 	1.371(7)

C(28)-C(29) 	1.393(8)

C(29)-C(30) 	1.329(8)

C(30)-C(31) 	1.360(9)

C(31)-C(32) 	1.365(8)

C(33)-C(34) 	1.310(8)

C(33)-C(38) 	1.327(8)

C(34)-C(35) 	1.391(9)

C(35)-C(36) 	1.298(9)

C(36)-C(37) 	1.313(9)

C(37)-C(38) 	1.402(9)

C(39)-C(44) 	1.345(8)

C(39)-C(40) 	1.375(8)

C(40)-C(41) 	1.388(9)

C(41)-C(42) 	1.343(10)

C(42)-C(43) 	1.349(10)

C(43)-C(44) 	1.379(8)

O(1)-C(48) 	1.433(17)

O(1)-C(45) 	1.510(14)

C(45)-C(46) 	1.428(15)

C(46)-C(47) 	1.350(17)

C(47)-C(48) 	1.263(19)

N(2)-Fe(1)-N(3)	87.7(2)

N(2)-Fe(1)-N(1)	88.5(2)

N(3)-Fe(1)-N(1)	144.69(18)

N(2)-Fe(1)-N(4)#1	110.32(17)

N(3)-Fe(1)-N(4)#1	95.30(18)

N(1)-Fe(1)-N(4)#1	118.83(18)

N(2)-Fe(1)-C(17)	143.4(2)

N(3)-Fe(1)-C(17)	81.1(2)

N(1)-Fe(1)-C(17)	81.3(2)

N(4)#1-Fe(1)-C(17)	105.38(18)

C(4)-N(1)-C(1)	105.3(5)

C(4)-N(1)-Fe(1)	122.8(4)

C(1)-N(1)-Fe(1)	131.1(4)

C(6)-N(2)-C(9)	105.2(5)

C(6)-N(2)-Fe(1)	126.1(4)

C(9)-N(2)-Fe(1)	127.1(4)

C(11)-N(3)-C(14)	105.1(5)

C(11)-N(3)-Fe(1)	125.1(4)

C(14)-N(3)-Fe(1)	129.1(4)

C(19)-N(4)-C(16)	98.7(5)

C(19)-N(4)-Fe(1)#1	113.0(4)

C(16)-N(4)-Fe(1)#1	127.9(4)

C(20)-C(1)-N(1)	125.8(6)

C(20)-C(1)-C(2)	124.5(6)

N(1)-C(1)-C(2)	109.7(5)

C(3)-C(2)-C(1)	107.5(6)

C(2)-C(3)-C(4)	107.4(6)

N(1)-C(4)-C(5)	126.5(6)

N(1)-C(4)-C(3)	110.0(6)

C(5)-C(4)-C(3)	123.5(6)

C(6)-C(5)-C(4)	124.7(6)

C(6)-C(5)-C(39)	118.5(6)

C(4)-C(5)-C(39)	116.6(6)

N(2)-C(6)-C(5)	124.5(6)

N(2)-C(6)-C(7)	110.0(6)

C(5)-C(6)-C(7)	125.3(7)

C(8)-C(7)-C(6)	108.2(6)

C(7)-C(8)-C(9)	106.5(6)

N(2)-C(9)-C(10)	124.6(6)

N(2)-C(9)-C(8)	110.0(6)

C(10)-C(9)-C(8)	125.4(7)

C(9)-C(10)-C(11)	125.8(6)

C(9)-C(10)-C(21)	118.3(6)

C(11)-C(10)-C(21)	115.9(6)

N(3)-C(11)-C(10)	125.1(6)

N(3)-C(11)-C(12)	110.2(6)

C(10)-C(11)-C(12)	124.6(7)

C(13)-C(12)-C(11)	106.8(6)

C(12)-C(13)-C(14)	109.0(6)

C(15)-C(14)-C(13)	126.9(6)

C(15)-C(14)-N(3)	124.1(6)

C(13)-C(14)-N(3)	108.8(6)

C(14)-C(15)-C(16)	120.6(6)

C(14)-C(15)-C(27)	119.9(6)

C(16)-C(15)-C(27)	119.4(6)

C(17)-C(16)-N(4)	114.0(5)

C(17)-C(16)-C(15)	125.8(6)

N(4)-C(16)-C(15)	120.1(6)

C(18)-C(17)-C(16)	107.3(5)

C(18)-C(17)-Fe(1)	111.7(4)

C(16)-C(17)-Fe(1)	107.1(4)

C(17)-C(18)-C(19)	103.3(5)

C(17)-C(18)-C(20)	129.4(6)

C(19)-C(18)-C(20)	126.5(6)

N(4)-C(19)-C(18)	115.9(6)

C(1)-C(20)-C(18)	120.0(6)

C(1)-C(20)-C(33)	122.1(6)

C(18)-C(20)-C(33)	117.8(6)

C(22)-C(21)-C(26)	117.3(8)

C(22)-C(21)-C(10)	121.6(9)

C(26)-C(21)-C(10)	121.2(8)

C(21)-C(22)-C(23)	120.9(10)

C(24)-C(23)-C(22)	121.9(14)

C(23)-C(24)-C(25)	121.1(15)

C(24)-C(25)-C(26)	116.6(12)

C(21)-C(26)-C(25)	122.2(9)

C(28)-C(27)-C(32)	118.7(6)

C(28)-C(27)-C(15)	123.9(6)

C(32)-C(27)-C(15)	117.4(7)

C(27)-C(28)-C(29)	118.9(7)

C(30)-C(29)-C(28)	121.5(8)

C(29)-C(30)-C(31)	120.1(9)

C(30)-C(31)-C(32)	119.3(8)

C(31)-C(32)-C(27)	121.4(7)

C(34)-C(33)-C(38)	113.5(7)

C(34)-C(33)-C(20)	122.2(8)

C(38)-C(33)-C(20)	124.2(7)

C(33)-C(34)-C(35)	123.7(8)

C(36)-C(35)-C(34)	121.5(9)

C(35)-C(36)-C(37)	117.4(9)

C(36)-C(37)-C(38)	120.0(9)

C(33)-C(38)-C(37)	123.7(8)

C(44)-C(39)-C(40)	118.8(7)

C(44)-C(39)-C(5)	122.5(7)

C(40)-C(39)-C(5)	118.6(7)

C(39)-C(40)-C(41)	119.3(8)

C(42)-C(41)-C(40)	120.1(10)

C(41)-C(42)-C(43)	121.2(11)

C(42)-C(43)-C(44)	118.5(9)

C(39)-C(44)-C(43)	122.0(8)

C(48)-O(1)-C(45)	96.9(13)

C(46)-C(45)-O(1)	105.4(12)

C(47)-C(46)-C(45)	96.7(13)

C(48)-C(47)-C(46)	104.2(16)

C(47)-C(48)-O(1)	104.4(17)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+2,-y,-z+1

Table 4.   Anisotropic displacement parameters  (Å2x 103) for h200m.  The anisotropic

displacement factor exponent takes the form:  -22[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Fe(1)	93(1) 	69(1)	58(1) 	-1(1)	-5(1) 	16(1)

N(1)	76(4) 	53(3)	53(3) 	-2(3)	-2(3) 	-6(3)

N(2)	67(4) 	56(3)	58(4) 	4(3)	-2(3) 	1(3)

N(3)	58(4) 	64(4)	66(4) 	1(3)	4(3) 	-2(3)

N(4)	48(3) 	41(3)	70(3) 	-5(3)	4(3) 	9(3)

C(1)	82(5) 	51(4)	59(4) 	1(4)	-9(4) 	-2(4)

C(2)	101(6) 	58(4)	81(5) 	11(4)	-16(5) 	7(4)

C(3)	100(6) 	63(5)	68(5) 	7(4)	-11(4) 	-1(4)

C(4)	61(5) 	71(5)	59(4) 	15(4)	-3(4) 	2(4)

C(5)	77(5) 	67(5)	56(4) 	-3(4)	3(4) 	4(4)

C(6)	79(5) 	63(5)	58(4) 	-4(4)	0(4) 	-3(4)

C(7)	93(6) 	69(5)	61(4) 	-8(4)	0(4) 	-4(4)

C(8)	96(6) 	63(5)	70(5) 	-12(4)	-7(4) 	9(4)

C(9)	73(5) 	65(5)	57(5) 	1(4)	2(4) 	-2(4)

C(10)	68(5) 	61(5)	67(5) 	-5(4)	6(4) 	5(4)

C(11)	64(5) 	58(5)	76(5) 	4(4)	-8(4) 	8(4)

C(12)	84(6) 	72(5)	82(5) 	-2(4)	-4(5) 	18(4)

C(13)	77(5) 	76(5)	63(5) 	2(4)	-7(4) 	10(4)

C(14)	58(5) 	66(5)	56(5) 	12(4)	-6(4) 	2(4)

C(15)	60(4) 	60(4)	55(4) 	4(4)	-5(4) 	-2(4)

C(16)	58(5) 	62(5)	63(5) 	5(4)	-7(4) 	-2(4)

C(17)	78(5) 	53(4)	53(4) 	-4(3)	-4(4) 	17(4)

C(18)	66(5) 	48(4)	51(4) 	2(3)	0(4) 	-9(4)

C(19)	92(6) 	72(5)	77(5) 	-10(4)	12(4) 	7(4)

C(20)	70(5) 	40(4)	77(5) 	19(4)	4(4) 	-11(3)

C(21)	80(6) 	77(6)	85(6) 	-4(5)	-13(5) 	14(5)

C(22)	172(10) 	128(8)	125(8) 	12(6)	39(7) 	78(7)

C(23)	254(15) 	182(12)	117(9) 	6(9)	24(9) 	126(13)

C(24)	217(16) 	116(10)	128(12) 	-60(8)	-92(11) 	79(11)

C(25)	182(12) 	76(8)	206(13) 	1(8)	-31(9) 	18(8)

C(26)	144(8) 	73(6)	197(10) 	5(7)	5(7) 	26(6)

C(27)	69(5) 	56(4)	72(5) 	-6(4)	-12(4) 	6(4)

C(28)	84(5) 	84(5)	65(5) 	10(4)	-9(4) 	0(4)

C(29)	103(7) 	129(8)	71(6) 	17(5)	-8(5) 	14(6)

C(30)	113(8) 	144(9)	77(6) 	-13(6)	-30(6) 	22(7)

C(31)	149(8) 	117(8)	125(8) 	-25(6)	-71(7) 	-17(6)

C(32)	116(7) 	92(6)	94(6) 	6(5)	-32(5) 	-16(5)

C(33)	79(6) 	58(5)	68(4) 	-2(4)	-11(4) 	5(5)

C(34)	125(8) 	63(6)	251(10) 	-49(6)	-58(7) 	7(6)

C(35)	126(9) 	62(7)	286(13) 	-32(7)	-37(9) 	-4(6)

C(36)	139(9) 	57(6)	126(6) 	-13(5)	-28(7) 	13(7)

C(37)	109(8) 	72(6)	281(13) 	-32(7)	7(8) 	23(6)

C(38)	88(7) 	71(6)	257(12) 	-32(6)	7(7) 	-7(5)

C(39)	87(6) 	76(5)	54(5) 	-2(4)	-16(5) 	3(4)

C(40)	103(7) 	110(6)	70(6) 	-14(5)	-22(5) 	-5(5)

C(41)	115(8) 	106(7)	130(9) 	-25(7)	-40(8) 	11(6)

C(42)	200(13) 	89(8)	86(7) 	-17(5)	-65(8) 	23(8)

C(43)	172(10) 	117(7)	63(6) 	1(5)	-14(6) 	8(7)

C(44)	123(7) 	109(6)	50(5) 	11(4)	-13(5) 	-8(5)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for h200m.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(2A)	10379	-1964	7028	96

H(3A)	10516	-1159	7815	92

H(7A)	9724	1306	8072	89

H(8A)	8889	2068	7499	91

H(12A)	7298	1938	5428	95

H(13A)	7290	1188	4587	86

H(17A)	8712	-432	5776	73

H(19A)	10132	-1496	4699	96

H(22A)	7168	2014	7043	170

H(23A)	6569	3013	7162	221

H(24A)	7079	3870	6715	184

H(25A)	8130	3770	6005	185

H(26A)	8756	2758	5892	166

H(28A)	8279	1048	3794	93

H(29A)	7678	942	2855	121

H(30A)	7125	-2	2552	134

H(31A)	7177	-890	3164	156

H(32A)	7789	-807	4086	121

H(34A)	9018	-2480	5565	176

H(35A)	9374	-3534	5394	190

H(36A)	10698	-3880	5512	129

H(37A)	11694	-3145	5758	185

H(38A)	11310	-2099	5983	167

H(40A)	11440	502	7961	113

H(41A)	11992	408	8918	140

H(42A)	11210	-34	9658	150

H(43A)	9888	-419	9472	141

H(44A)	9358	-361	8516	113

H(45A)	147	2435	6199	348

H(45B)	274	2735	6840	348

H(46A)	807	3321	5942	348

H(46B)	1336	3341	6544	348

H(47A)	1418	2397	5687	413

H(47B)	2139	2899	5832	413

H(48A)	2174	2573	6737	426

H(48B)	2300	1984	6299	426

________________________________________________________________________________

Supporting Figure 5. Views of [Fe(NCTPP)]2 (6) with atomic labelling Scheme.  Thermal ellipsoids are scales to 35% probability level.

Crystal Structure Report for [Fe(NCOTPP)]2(OH)•Na(THF)2 (7)

Table 1.  Crystal data and structure refinement.

Table 2.  	Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103).

Table 3.   Bond lengths [Å] and angles [°].

Table 4.   Anisotropic displacement parameters  (Å2x 103)

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

Supporting Figure 6. Views of [Fe(NCOTPP)]2(OH)•Na(THF)2 (7)) with atomic labelling Scheme.  Thermal ellipsoids are scales to 35% probability level.

Table 1.  Crystal data and structure refinement for h313m.

Identification code 	h313m

Empirical formula 	C108 H95 Fe2 N8 Na O8

Formula weight 	1767.61

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 28.473(3) Å	= 90°.

b = 18.7702(18) Å	= 104.922(2)°.

c = 16.8963(16) Å	 = 90°.

Volume	8725.6(14) Å3

Z	4

Density (calculated)	1.346 Mg/m3

Absorption coefficient	0.404 mm-1

F(000)	3704

Crystal size	0.38 x 0.14 x 0.10 mm3

Theta range for data collection	1.31 to 25.02°.

Index ranges	-33<=h<=23, -22<=k<=22, -19<=l<=20

Reflections collected	24722

Independent reflections	7695 [R(int) = 0.0936]

Completeness to theta = 25.02°	99.8 %

Absorption correction	Empirical Used SADABS

Max. and min. transmission	0.9486 and 0.6301

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	7695 / 0 / 578

Goodness-of-fit on F2	0.924

Final R indices [I>2sigma(I)]	R1 = 0.0702, wR2 = 0.1815

R indices (all data)	R1 = 0.1538, wR2 = 0.2238

Largest diff. peak and hole	1.392 and -0.822 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103)

for h313m.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Fe(1)	9893(1)	6895(1)	3531(1)	34(1)

O(1)	10000	6565(3)	2500	44(1)

O(2)	9922(2)	6348(2)	4529(2)	44(1)

N(1)	10611(2)	7182(2)	4113(3)	35(1)

N(2)	9697(2)	7929(2)	3505(3)	33(1)

N(3)	9162(2)	6590(2)	3208(3)	35(1)

N(4)	10035(2)	4704(3)	3493(3)	40(1)

C(1)	10998(2)	6733(3)	4469(3)	37(1)

C(2)	11399(2)	7144(3)	4911(3)	40(2)

C(3)	11269(2)	7833(3)	4817(3)	38(1)

C(4)	10780(2)	7859(3)	4314(3)	35(1)

C(5)	10505(2)	8485(3)	4065(3)	32(1)

C(6)	10015(2)	8511(3)	3661(3)	32(1)

C(7)	9745(2)	9140(3)	3359(3)	32(1)

C(8)	9278(2)	8950(3)	3033(3)	34(1)

C(9)	9242(2)	8190(3)	3127(3)	32(1)

C(10)	8809(2)	7799(3)	2912(3)	33(1)

C(11)	8770(2)	7045(3)	2997(3)	36(1)

C(12)	8324(2)	6658(3)	2881(3)	40(1)

C(13)	8450(2)	5964(3)	3024(3)	41(2)

C(14)	8967(2)	5912(3)	3217(3)	36(1)

C(15)	9244(2)	5270(3)	3351(3)	36(1)

C(16)	9745(2)	5271(3)	3671(3)	37(1)

C(17)	10058(2)	5797(3)	4139(3)	37(1)

C(18)	10544(2)	5593(3)	4169(3)	35(1)

C(19)	10489(2)	4906(3)	3783(3)	39(1)

C(20)	10982(2)	5975(3)	4426(3)	37(1)

C(21)	10767(2)	9177(3)	4270(3)	35(1)

C(22)	11181(2)	9330(3)	4009(3)	37(1)

C(23)	11435(2)	9962(3)	4212(3)	43(2)

C(24)	11279(2)	10463(3)	4692(4)	47(2)

C(25)	10870(2)	10319(3)	4959(3)	46(2)

C(26)	10619(2)	9690(3)	4756(3)	41(2)

C(27)	8346(2)	8191(3)	2547(3)	34(1)

C(28)	8090(2)	8053(3)	1745(3)	40(1)

C(29)	7672(2)	8430(4)	1381(4)	51(2)

C(30)	7496(2)	8931(4)	1808(5)	60(2)

C(31)	7740(2)	9075(4)	2602(5)	57(2)

C(32)	8166(2)	8702(3)	2982(4)	46(2)

C(33)	8995(2)	4585(3)	3089(3)	35(1)

C(34)	8646(2)	4512(3)	2332(3)	43(2)

C(35)	8429(2)	3858(3)	2088(4)	50(2)

C(36)	8546(2)	3270(3)	2577(4)	50(2)

C(37)	8894(3)	3332(3)	3322(4)	51(2)

C(38)	9114(2)	3973(3)	3582(3)	40(2)

C(39)	11450(2)	5572(3)	4614(3)	39(1)

C(40)	11490(2)	4937(3)	5055(3)	44(2)

C(41)	11913(3)	4533(3)	5180(4)	54(2)

C(42)	12291(3)	4765(4)	4871(4)	58(2)

C(43)	12255(2)	5388(4)	4452(4)	51(2)

C(44)	11833(2)	5790(3)	4313(4)	45(2)

Na(1)	10000	3767(2)	2500	83(1)

O(4)	10377(2)	2921(3)	3449(3)	99(2)

C(45)	10763(4)	3037(5)	4170(6)	110(3)

C(46)	10775(4)	2409(5)	4698(5)	90(3)

C(47)	10263(5)	2106(6)	4370(6)	119(4)

C(48)	10071(5)	2403(9)	3643(9)	242(11)

O(5)	1707(5)	1438(5)	2830(7)	225(6)

C(49)	1165(5)	1288(8)	2551(7)	170(6)

C(50)	997(7)	1114(6)	1731(7)	252(12)

C(51)	1543(5)	813(7)	1645(8)	152(5)

C(52)	1955(5)	1226(8)	2153(11)	234(10)

C(54)	7393(4)	2581(5)	629(7)	102(3)

O(3)	7176(5)	3112(7)	163(8)	103(4)

C(53)	7823(4)	2254(8)	507(7)	140(5)

________________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [°] for  h313m.

_____________________________________________________

Fe(1)-O(1) 	1.945(2)

Fe(1)-O(2) 	1.957(4)

Fe(1)-N(2) 	2.017(4)

Fe(1)-N(3) 	2.093(5)

Fe(1)-N(1) 	2.098(5)

Fe(1)-C(17) 	2.296(5)

O(1)-Fe(1)#1 	1.945(2)

O(2)-C(17) 	1.336(6)

N(1)-C(4) 	1.369(7)

N(1)-C(1) 	1.394(7)

N(2)-C(9) 	1.378(7)

N(2)-C(6) 	1.398(7)

N(3)-C(11) 	1.376(7)

N(3)-C(14) 	1.389(7)

N(4)-C(19) 	1.315(7)

N(4)-C(16) 	1.427(7)

N(4)-Na(1) 	2.414(6)

C(1)-C(2) 	1.421(8)

C(1)-C(20) 	1.424(8)

C(2)-C(3) 	1.344(8)

C(3)-C(4) 	1.434(8)

C(4)-C(5) 	1.414(8)

C(5)-C(6) 	1.389(7)

C(5)-C(21) 	1.493(8)

C(6)-C(7) 	1.430(7)

C(7)-C(8) 	1.348(7)

C(8)-C(9) 	1.441(7)

C(9)-C(10) 	1.400(7)

C(10)-C(11) 	1.431(8)

C(10)-C(27) 	1.497(8)

C(11)-C(12) 	1.433(8)

C(12)-C(13) 	1.357(8)

C(13)-C(14) 	1.427(8)

C(14)-C(15) 	1.426(8)

C(15)-C(16) 	1.389(8)

C(15)-C(33) 	1.479(8)

C(16)-C(17) 	1.425(8)

C(17)-C(18) 	1.425(8)

C(18)-C(20) 	1.406(8)

C(18)-C(19) 	1.437(8)

C(19)-Na(1) 	3.106(6)

C(20)-C(39) 	1.495(8)

C(21)-C(22) 	1.392(8)

C(21)-C(26) 	1.399(7)

C(22)-C(23) 	1.385(8)

C(23)-C(24) 	1.388(8)

C(24)-C(25) 	1.382(8)

C(25)-C(26) 	1.375(8)

C(27)-C(32) 	1.385(8)

C(27)-C(28) 	1.388(8)

C(28)-C(29) 	1.384(8)

C(29)-C(30) 	1.358(9)

C(30)-C(31) 	1.371(9)

C(31)-C(32) 	1.405(9)

C(33)-C(38) 	1.409(8)

C(33)-C(34) 	1.410(8)

C(34)-C(35) 	1.388(8)

C(35)-C(36) 	1.367(8)

C(36)-C(37) 	1.393(9)

C(37)-C(38) 	1.376(8)

C(39)-C(44) 	1.378(8)

C(39)-C(40) 	1.395(8)

C(40)-C(41) 	1.393(8)

C(41)-C(42) 	1.381(9)

C(42)-C(43) 	1.357(9)

C(43)-C(44) 	1.387(8)

Na(1)-O(4)#1 	2.315(6)

Na(1)-O(4) 	2.315(6)

Na(1)-N(4)#1 	2.414(6)

Na(1)-C(19)#1 	3.106(6)

O(4)-C(48) 	1.400(12)

O(4)-C(45) 	1.430(10)

C(45)-C(46) 	1.472(11)

C(46)-C(47) 	1.528(13)

C(47)-C(48) 	1.331(13)

O(5)-C(49) 	1.522(16)

O(5)-C(52) 	1.544(18)

C(49)-C(50) 	1.384(14)

C(50)-C(51) 	1.69(2)

C(51)-C(52) 	1.483(15)

C(54)-O(3) 	1.319(14)

C(54)-C(53) 	1.431(14)

C(54)-C(53)#2 	1.883(15)

O(3)-C(53)#2 	1.325(15)

C(53)-O(3)#2 	1.325(15)

C(53)-C(54)#2 	1.883(15)

O(1)-Fe(1)-O(2)	128.6(2)

O(1)-Fe(1)-N(2)	113.1(2)

O(2)-Fe(1)-N(2)	118.27(17)

O(1)-Fe(1)-N(3)	93.10(13)

O(2)-Fe(1)-N(3)	84.23(17)

N(2)-Fe(1)-N(3)	90.40(18)

O(1)-Fe(1)-N(1)	98.20(13)

O(2)-Fe(1)-N(1)	84.92(17)

N(2)-Fe(1)-N(1)	89.64(18)

N(3)-Fe(1)-N(1)	167.69(17)

O(1)-Fe(1)-C(17)	93.1(2)

O(2)-Fe(1)-C(17)	35.49(17)

N(2)-Fe(1)-C(17)	153.76(19)

N(3)-Fe(1)-C(17)	86.89(19)

N(1)-Fe(1)-C(17)	87.64(19)

Fe(1)#1-O(1)-Fe(1)	142.9(3)

C(17)-O(2)-Fe(1)	86.2(3)

C(4)-N(1)-C(1)	105.5(5)

C(4)-N(1)-Fe(1)	126.2(4)

C(1)-N(1)-Fe(1)	127.8(4)

C(9)-N(2)-C(6)	107.1(4)

C(9)-N(2)-Fe(1)	125.0(4)

C(6)-N(2)-Fe(1)	125.8(4)

C(11)-N(3)-C(14)	105.8(5)

C(11)-N(3)-Fe(1)	125.6(4)

C(14)-N(3)-Fe(1)	128.4(4)

C(19)-N(4)-C(16)	105.9(5)

C(19)-N(4)-Na(1)	109.2(4)

C(16)-N(4)-Na(1)	140.1(4)

N(1)-C(1)-C(2)	109.7(5)

N(1)-C(1)-C(20)	124.8(5)

C(2)-C(1)-C(20)	125.5(5)

C(3)-C(2)-C(1)	107.5(5)

C(2)-C(3)-C(4)	107.3(5)

N(1)-C(4)-C(5)	124.5(5)

N(1)-C(4)-C(3)	109.9(5)

C(5)-C(4)-C(3)	125.6(5)

C(6)-C(5)-C(4)	125.7(5)

C(6)-C(5)-C(21)	117.5(5)

C(4)-C(5)-C(21)	116.7(5)

C(5)-C(6)-N(2)	125.8(5)

C(5)-C(6)-C(7)	125.8(5)

N(2)-C(6)-C(7)	108.4(5)

C(8)-C(7)-C(6)	108.1(5)

C(7)-C(8)-C(9)	107.9(5)

N(2)-C(9)-C(10)	126.5(5)

N(2)-C(9)-C(8)	108.6(5)

C(10)-C(9)-C(8)	124.9(5)

C(9)-C(10)-C(11)	125.3(5)

C(9)-C(10)-C(27)	118.3(5)

C(11)-C(10)-C(27)	116.4(5)

N(3)-C(11)-C(10)	124.2(5)

N(3)-C(11)-C(12)	110.6(5)

C(10)-C(11)-C(12)	125.2(5)

C(13)-C(12)-C(11)	106.1(5)

C(12)-C(13)-C(14)	108.4(5)

N(3)-C(14)-C(15)	124.7(5)

N(3)-C(14)-C(13)	109.1(5)

C(15)-C(14)-C(13)	126.2(5)

C(16)-C(15)-C(14)	122.1(5)

C(16)-C(15)-C(33)	118.8(5)

C(14)-C(15)-C(33)	119.0(5)

C(15)-C(16)-C(17)	130.6(5)

C(15)-C(16)-N(4)	120.6(5)

C(17)-C(16)-N(4)	108.7(5)

O(2)-C(17)-C(16)	126.2(5)

O(2)-C(17)-C(18)	126.3(5)

C(16)-C(17)-C(18)	107.3(5)

O(2)-C(17)-Fe(1)	58.3(3)

C(16)-C(17)-Fe(1)	110.3(4)

C(18)-C(17)-Fe(1)	110.0(4)

C(20)-C(18)-C(17)	130.5(5)

C(20)-C(18)-C(19)	125.7(5)

C(17)-C(18)-C(19)	103.5(5)

N(4)-C(19)-C(18)	114.2(5)

N(4)-C(19)-Na(1)	47.2(3)

C(18)-C(19)-Na(1)	155.8(4)

C(18)-C(20)-C(1)	122.6(5)

C(18)-C(20)-C(39)	118.6(5)

C(1)-C(20)-C(39)	118.7(5)

C(22)-C(21)-C(26)	116.8(5)

C(22)-C(21)-C(5)	121.2(5)

C(26)-C(21)-C(5)	122.0(5)

C(23)-C(22)-C(21)	122.0(5)

C(22)-C(23)-C(24)	120.1(6)

C(25)-C(24)-C(23)	118.8(6)

C(26)-C(25)-C(24)	120.9(6)

C(25)-C(26)-C(21)	121.6(6)

C(32)-C(27)-C(28)	118.3(6)

C(32)-C(27)-C(10)	121.9(5)

C(28)-C(27)-C(10)	119.8(5)

C(29)-C(28)-C(27)	120.9(6)

C(30)-C(29)-C(28)	120.8(6)

C(29)-C(30)-C(31)	119.5(6)

C(30)-C(31)-C(32)	120.7(7)

C(27)-C(32)-C(31)	119.8(6)

C(38)-C(33)-C(34)	117.6(5)

C(38)-C(33)-C(15)	120.6(5)

C(34)-C(33)-C(15)	121.9(5)

C(35)-C(34)-C(33)	120.8(6)

C(36)-C(35)-C(34)	120.9(6)

C(35)-C(36)-C(37)	119.0(6)

C(38)-C(37)-C(36)	121.4(6)

C(37)-C(38)-C(33)	120.3(6)

C(44)-C(39)-C(40)	119.2(6)

C(44)-C(39)-C(20)	121.2(5)

C(40)-C(39)-C(20)	119.4(5)

C(41)-C(40)-C(39)	119.6(6)

C(42)-C(41)-C(40)	119.9(6)

C(43)-C(42)-C(41)	120.5(6)

C(42)-C(43)-C(44)	120.3(7)

C(39)-C(44)-C(43)	120.5(6)

O(4)#1-Na(1)-O(4)	93.4(3)

O(4)#1-Na(1)-N(4)	155.4(2)

O(4)-Na(1)-N(4)	95.13(18)

O(4)#1-Na(1)-N(4)#1	95.13(18)

O(4)-Na(1)-N(4)#1	155.4(2)

N(4)-Na(1)-N(4)#1	86.6(2)

O(4)#1-Na(1)-C(19)	179.0(2)

O(4)-Na(1)-C(19)	86.79(18)

N(4)-Na(1)-C(19)	23.56(15)

N(4)#1-Na(1)-C(19)	85.14(18)

O(4)#1-Na(1)-C(19)#1	86.79(18)

O(4)-Na(1)-C(19)#1	179.0(2)

N(4)-Na(1)-C(19)#1	85.14(18)

N(4)#1-Na(1)-C(19)#1	23.56(15)

C(19)-Na(1)-C(19)#1	93.1(2)

C(48)-O(4)-C(45)	107.0(8)

C(48)-O(4)-Na(1)	115.7(7)

C(45)-O(4)-Na(1)	127.1(5)

O(4)-C(45)-C(46)	106.7(8)

C(45)-C(46)-C(47)	102.0(8)

C(48)-C(47)-C(46)	107.8(9)

C(47)-C(48)-O(4)	112.0(11)

C(49)-O(5)-C(52)	110.1(9)

C(50)-C(49)-O(5)	114.5(15)

C(49)-C(50)-C(51)	94.4(12)

C(52)-C(51)-C(50)	112.5(11)

C(51)-C(52)-O(5)	96.8(11)

O(3)-C(54)-C(53)	121.5(11)

O(3)-C(54)-C(53)#2	44.7(7)

C(53)-C(54)-C(53)#2	89.4(8)

C(54)-O(3)-C(53)#2	90.8(11)

O(3)#2-C(53)-C(54)	122.4(11)

O(3)#2-C(53)-C(54)#2	44.4(7)

C(54)-C(53)-C(54)#2	90.6(8)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+2,y,-z+1/2    #2 -x+3/2,-y+1/2,-z

Table 4.   Anisotropic displacement parameters  (Å2x 103) for h313m.  The anisotropic

displacement factor exponent takes the form:  -22[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Fe(1)	30(1) 	34(1)	37(1) 	2(1)	6(1) 	2(1)

O(1)	44(4) 	46(3)	40(3) 	0	8(3) 	0

O(2)	44(3) 	44(2)	42(2) 	0(2)	9(2) 	-1(2)

N(1)	34(3) 	36(3)	36(3) 	2(2)	7(2) 	2(2)

N(2)	23(3) 	35(3)	38(3) 	4(2)	4(2) 	-1(2)

N(3)	36(3) 	35(3)	34(3) 	5(2)	8(2) 	2(2)

N(4)	42(4) 	41(3)	38(3) 	7(2)	10(2) 	7(3)

C(1)	30(3) 	44(4)	34(3) 	2(3)	6(3) 	5(3)

C(2)	29(4) 	44(4)	43(3) 	-1(3)	3(3) 	7(3)

C(3)	34(4) 	40(4)	37(3) 	0(3)	4(3) 	-2(3)

C(4)	29(3) 	40(4)	36(3) 	1(3)	6(3) 	0(3)

C(5)	28(4) 	39(3)	29(3) 	2(3)	9(2) 	1(3)

C(6)	30(4) 	36(3)	30(3) 	-4(3)	9(3) 	4(3)

C(7)	30(4) 	35(3)	34(3) 	0(3)	11(3) 	2(3)

C(8)	32(4) 	36(3)	34(3) 	4(3)	8(3) 	3(3)

C(9)	24(3) 	36(3)	37(3) 	-1(3)	8(2) 	5(3)

C(10)	28(3) 	35(3)	36(3) 	4(3)	6(2) 	3(3)

C(11)	28(3) 	41(4)	36(3) 	4(3)	4(2) 	1(3)

C(12)	33(4) 	46(4)	39(3) 	5(3)	8(3) 	1(3)

C(13)	34(4) 	44(4)	46(3) 	3(3)	11(3) 	-3(3)

C(14)	36(4) 	35(4)	37(3) 	2(3)	9(3) 	-3(3)

C(15)	35(4) 	36(3)	39(3) 	5(3)	13(3) 	-4(3)

C(16)	40(4) 	35(3)	37(3) 	6(3)	13(3) 	2(3)

C(17)	40(4) 	33(3)	37(3) 	3(3)	7(3) 	1(3)

C(18)	32(4) 	37(3)	38(3) 	4(3)	9(3) 	1(3)

C(19)	39(4) 	42(4)	37(3) 	2(3)	12(3) 	7(3)

C(20)	36(4) 	41(4)	31(3) 	5(3)	6(3) 	5(3)

C(21)	31(3) 	40(3)	32(3) 	2(3)	2(2) 	7(3)

C(22)	34(4) 	41(3)	34(3) 	-2(3)	8(3) 	1(3)

C(23)	32(4) 	50(4)	47(3) 	-2(3)	11(3) 	-3(3)

C(24)	44(4) 	42(4)	55(4) 	-9(3)	10(3) 	-9(3)

C(25)	53(4) 	41(4)	43(3) 	-10(3)	12(3) 	1(3)

C(26)	38(4) 	43(4)	43(3) 	-7(3)	16(3) 	1(3)

C(27)	26(3) 	35(3)	41(3) 	7(3)	9(3) 	-4(3)

C(28)	28(3) 	51(4)	43(3) 	6(3)	11(3) 	-1(3)

C(29)	28(4) 	67(5)	50(4) 	14(4)	0(3) 	-5(3)

C(30)	27(4) 	56(5)	90(6) 	25(4)	0(4) 	1(3)

C(31)	39(4) 	54(4)	81(5) 	2(4)	21(4) 	9(4)

C(32)	35(4) 	48(4)	55(4) 	0(3)	9(3) 	1(3)

C(33)	31(4) 	35(3)	40(3) 	0(3)	12(3) 	-1(3)

C(34)	43(4) 	47(4)	43(3) 	3(3)	16(3) 	-4(3)

C(35)	47(4) 	54(4)	47(4) 	-4(3)	9(3) 	-16(3)

C(36)	51(4) 	44(4)	57(4) 	-7(3)	16(3) 	-18(3)

C(37)	69(5) 	33(4)	58(4) 	4(3)	28(4) 	-3(3)

C(38)	47(4) 	39(4)	35(3) 	2(3)	13(3) 	-3(3)

C(39)	38(4) 	37(3)	39(3) 	-6(3)	6(3) 	6(3)

C(40)	43(4) 	40(4)	42(3) 	0(3)	1(3) 	11(3)

C(41)	57(5) 	41(4)	53(4) 	-9(3)	-7(3) 	13(4)

C(42)	39(5) 	56(5)	71(5) 	-18(4)	-2(4) 	8(4)

C(43)	31(4) 	59(5)	62(4) 	-23(4)	8(3) 	-1(3)

C(44)	40(4) 	45(4)	48(3) 	-11(3)	7(3) 	-3(3)

Na(1)	115(4) 	61(3)	61(2) 	0	1(2) 	0

O(4)	119(6) 	87(4)	77(4) 	19(3)	2(4) 	3(4)

C(45)	109(9) 	108(8)	102(8) 	35(6)	9(6) 	1(7)

C(46)	114(8) 	95(7)	69(5) 	28(5)	38(5) 	25(6)

C(47)	156(11) 	124(9)	83(7) 	21(6)	43(7) 	-29(8)

C(48)	120(12) 	340(20)	246(18) 	236(18)	7(11) 	-37(13)

O(5)	256(13) 	126(7)	215(11) 	-85(7)	-77(9) 	41(8)

C(49)	170(14) 	191(14)	99(9) 	20(9)	-55(8) 	-64(11)

C(50)	460(30) 	84(8)	114(10) 	-44(7)	-103(14) 	117(13)

C(51)	132(12) 	135(11)	156(12) 	13(9)	-21(9) 	26(9)

C(52)	103(11) 	203(15)	370(20) 	-223(17)	6(13) 	15(10)

C(54)	124(9) 	79(7)	115(8) 	-7(6)	52(7) 	-3(6)

O(3)	110(11) 	98(10)	92(9) 	-5(8)	9(8) 	17(8)

C(53)	116(10) 	207(14)	93(8) 	-52(8)	19(7) 	24(9)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for h313m.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1A)	10000	6070	2500	52

H(2)	11697	6968	5211	48

H(3)	11461	8222	5036	45

H(7)	9869	9600	3384	39

H(8)	9025	9255	2790	41

H(12)	8011	6845	2737	47

H(13)	8235	5586	3000	50

H(19A)	10752	4627	3741	47

H(22)	11291	8998	3689	44

H(23)	11709	10050	4026	51

H(24)	11448	10889	4831	57

H(25)	10762	10651	5281	55

H(26)	10345	9605	4945	49

H(28)	8200	7702	1448	48

H(29)	7511	8339	838	61

H(30)	7211	9175	1562	72

H(31)	7623	9423	2893	69

H(32)	8327	8799	3523	56

H(34)	8560	4906	1992	52

H(35)	8201	3820	1586	60

H(36)	8395	2835	2413	60

H(37)	8980	2931	3651	61

H(38)	9342	4002	4086	48

H(40)	11235	4784	5263	52

H(41)	11942	4108	5472	65

H(42)	12572	4492	4950	70

H(43)	12514	5545	4258	61

H(44)	11809	6211	4015	54

H(45A)	10703	3466	4449	132

H(45B)	11070	3089	4028	132

H(46A)	10834	2545	5269	108

H(46B)	11021	2071	4638	108

H(47A)	10278	1593	4314	143

H(47B)	10066	2213	4744	143

H(48A)	9763	2621	3647	291

H(48B)	10009	2037	3225	291

H(49A)	1089	899	2876	204

H(49B)	990	1706	2660	204

H(50A)	883	1525	1387	302

H(50B)	750	746	1632	302

H(51A)	1579	317	1810	182

H(51B)	1552	839	1076	182

H(52A)	2036	1637	1865	281

H(52B)	2242	935	2360	281

________________________________________________________________________________

Supporting Figure 6. Views of [Fe(NCOTPP)]2(OH)•Na(THF)2 (7) with atomic labelling Scheme.  Thermal ellipsoids are scales to 35% probability level.