The first organically templated 1-D lithioberyllofluoride chain, [LiBe2F7][C4N2H12][H2O]1.5

Lee A. Gerrard,* Mark T. Weller

Supplementary data.

TGA curve for title compound. Carried out in static air in the range 25 to 500 ºC (heating rate 10 ºC/min). Mass loss between 100-150 ºC is 10 % and is due to the solvent water and HF molecules. Second and third mass loss is due to each of the piperazine molecules at roughly 20 %.

IR showing the main stretches at 3587, 3443, 3247, 3022, 3005, 2872, 2820 and 2576 cm-1 for (O-H), (N-H) and (C-H).

# Metal-Metal distances

BE(1)   -  LI(1)    2.972(3)

BE(1)   -  LI(1)a   3.093(3)

BE(2)   -  LI(1)    3.022(3)

BE(2)   -  LI(1)b    3.058(3)

LI(1)   -  LI(1)a    3.994(3)

LI(1)   -  LI(1)b    4.085(4)

a = 1-x,1-y,1-z,  b = -x,1-y,1-z

# Hydrogen bonding distances

Table S9 - Hydrogen Bonds (Angstrom, Deg)

for: s92 in P-1

## D       H     A           D-H        H…A        D…A        D-H…A   Symmop-A

N1   -- H1 .. F7         0.90(2)    1.76(2)   2.622(2)     160(2)   2_656

N1   -- H2 .. F1         0.90(2)    1.90(2)   2.766(3)     162(2)   2_666

N2   -- H7 .. F2         0.86(2)    1.79(2)   2.630(2)     165(2)   2_666

N2   -- H8 .. F4         0.89(2)    1.94(2)   2.774(2)     155(2)   1_654

Translation of Symmetry Code to Equiv.Pos

[2666.00]  = 1-x,1-y,1-z

[2656.00]  = 1-x,-y,1-z

[1654.00]  = 1+x,y,-1+z

Synthetic details and analytical data

The title compound was synthesised by a two-step hydrothermal process followed by a slow evaporation. BeF2 (0.1 g), HF (0.17 ml) and C4N2H10 (0.18 g) were added to H2O (1 ml) in a 23 ml Teflon lined autoclave and heated to 150 C for 2 hr. The mix was then cooled for 3 hr and one equivalent of Li2CO3 (0.035 g) was added then reheated at 150 C for 1 day. After the resulting solution was left to cool and slowly evaporate colourless rod like single crystals were formed. Anal. Calc. for  Li2Be4F14C8N4H30O3; C 16.97; H 5.50; N 9.66 %; Found C 16.70; H 5.93; N 9.68 %. IR (cm–1): 3587w, 3443wb, 3247m, 3022m, 3005m, 2872w, 2820w, 2575w (O-H), (N-H) and (C-H) stretches.