# Supplementary Information

Fig. 4 Effect of oxygen on the conversion of CF4 over AlPO4-Al2O3 (Al/P = 39) (T= 640 oC, Catalyst = 5g, PFCs = 1.1 ml/min, He = 87 ml/min and water = 0.04 ml/min); this figure shows clearly that the hydrolysis activity is not influenced by the presence of oxygen.

Fig. 5. FTIR spectra of (a) Al2O3 and  (b) AlPO4-Al2O3(Al/P=39) after pyridine adsorption at ambient temperature and outgassing at 100 oC: (A) before and (B) after CF4 hydrolysis at 750 oC for 45 hours; this figure shows clearly that the hydrolysis activity is strongly influenced by the acidity of catalyst, which can be maintained even after long exposure to the reaction when the catalyst is promoted with phosphate.

Fresh

Used

(a) -Al2O3

(b) AlPO4-Al2O3 (Al/P=39)

Fig. 6. SEM images of (a) -Al2O3 and (b) AlPO4-Al2O3 (Al/P=39) before and after CF4 hydrolysis at 750C for 45 hours; in the case of pure -Al2O3, it showed an irregular shapes before reaction but converted to a hexagonal disk having a -phase of alumina after 45 hours of hydrolysis. On the contrary, the AlPO4-Al2O3 promoted with phosphate revealed no big change in morphology even after long exposure to the hydrolysis.