Figure 1 XRD pattern of TS-1 (reference)

Figure 2 XRD pattern of Ti-Sn-S-1 [1]

Figure 3 XRD pattern of Ti-Sn-S-1 [2]

Figure 4 XRD pattern of Ti-Sn-S-1 [3]

Note: XRD patterns were detected by a SCINTAG XDS 2000 theta-theta diffractometer, generating Cu tube K1 radiation with Peltier detector. A full scanning was performed between 2-70 o2, step size 0.02 o2, 1 sec/step with the slits: 0.3 nm, 0.5 nm, 2 nm and 4 nm.

Table 1 NH3-TPD summary results

| Catalyst | mmol of NH3 per gram in specified temperature region |  |  |  | Total mmol NH3 per gram 200 – 550 oC |
| --- | --- | --- | --- | --- | --- |
|  | 200 – 300 oC | 300 – 400 oC | 400 – 500 oC | 500 – 550 oC |  |
| TS-1 | 0.004 | 0.012 | 0.010 | 0.004 | 0.030 |
| Sn-S-1 | 0.022 | 0.026 | 0.017 | 0.007 | 0.072 |
| Ti-Sn-S-1 [1] | 0.006 | 0.015 | 0.014 | 0.005 | 0.040 |
| Ti-Sn-S-1 [2] | 0.007 | 0.018 | 0.017 | 0.006 | 0.049 |
| Ti-Sn-S-1 [3] | 0.036 | 0.040 | 0.022 | 0.008 | 0.106 |
| Sn on TS-1 | 0.006 | 0.015 | 0.011 | 0.004 | 0.036 |
| Ti on Sn-S-1 | 0.015 | 0.021 | 0.017 | 0.006 | 0.059 |

Note: All samples have been pretreated at 550 oC in UHP grade He

Table 2 Some characterization results

| Catalyst | Pore Volume (cc g -1) | Pore Diameter (Å) | Micropore Area (m2 g -1) | Micropore Volume (cc g -1) | Mesopore Area (m2 g -1) |
| --- | --- | --- | --- | --- | --- |
| TS-1 | 0.44 | 32.0 | 370.0 | 0.19 | 28.0 |
| Sn-S-1 | 0.46 | 40.0 | 287.0 | 0.16 | 169.0 |
| Ti-Sn-S-1 [1] | 0.40 | 40.0 | 365.0 | 0.20 | 38.0 |
| Ti-Sn-S-1 [2] | 0.40 | 39.0 | 323.0 | 0.20 | 101.5 |
| Ti-Sn-S-1 [3] | 0.43 | 38.0 | 281.0 | 0.20 | 165.0 |
| Sn on TS-1 | 0.32 | 32.0 | 371.0 | 0.20 | 29.0 |
| Ti on Sn-S-1 | 0.43 | 40.0 | 345.0 | 0.20 | 169.0 |

Note: All samples have been pretreated by N2 adsorption at 300 oC overnight