Supplementary material (ESI) for Chemical Communications

This journal is © The Royal Society of Chemistry 2003

Fig. S1 FTIR spectra showing the Si-O band shift due to the presence of Al-O-Si bonding. (A) Silica-gel@5%Pt on -alumina, Al/Si =18, (B) Silica-gel@5%Pt on -alumina, Al/Si=2, (C) Silica-gel@5%Pt, Al/Si=0, (D) Silica Gel, (E) -alumina support (F) Calcined Silica-gel@5%Pt on -alumina Al/Si=2.

As noted from the Figure S1, FTIR was used to characterize the linkages between the alumina support and aerogel@metal nano-composites before and after calcination. Figures S1(D) and S1(E) show the IR absorption spectra of pure silica gel and alumina support, respectively. Particularly, region from 1400 to 800 cm-1 where the dominant features of asymmetric vibration modes of Si-O(A) are closely examined. When A = Si (in pure silica), the corresponding asymmetric vibration is at about 1085 and when A= H (a large quantity of surface hydroxyl), the asymmetric vibration of Si-O(H) is at near 975cm-1 10. Thus, the position of this asymmetric vibration Si-O mode depends on the second neighbor atoms, which is generally accepted in sol-gel synthesis10 as the way to determine whether atomic mixing of Al into SiO2 matrix can be achieved as [Si-O-(Al)] during aging the Al and Si precursors together at room temperature via examining the shift in the wavelength. Substitution of Al amongst the Si-O network will attenuate the stretching wavenumber (due to Si-O(Al))10..It is believed that the presence of (Al3+) (a Lewis acid site of the size considerably smaller than Si) as the second neighbor of the Si-O, the (Al3+) will attract the oxygen more stronger than (Si). Hence, the Si-O(Al) asymmetric stretching would be located at a lower k value than Si-O(Si). Figure S1C and S1D represent those samples without the addition of alumina support. The Si-O(Si) asymmetric stretching bands located at ~1085cm-1 and Si-O(H) hydroyl groups stretching bands located at ~980cm-1 (a large quantity of terminal hydroxyl groups for these small sol-gel silica samples) are clearly visible. On the other hand, Figure S1A, S1B and S1F show clearly the disappearance of Si-O(H) hydroxyl groups stretching bands at ~980cm-1 associated with a progressive shift of the Si-O asymmetric stretching band to a lower wavenumbers on increasing the alumina support content. Thus, the presence and increasing degree of covalent linkages of the Si-O(Al) due to the condensation of the surface –OH group of the nanocomposites and the support (Al-OH) is therefore evident. It is noted that the well-dispersed alumina supported silogel coated nanocomposites with a high aluminum content (Al/Si = 18) accounts for more Si-O(Al) linkages consequence with a larger degree of shift. These are taken as evidence for the formation of chemical linkage between the sol-gel silica coating with the alumina support when the two materials were allowed to mix at room temperature for a prolonged period of time. It is also noted that Figure S1F represents the Silica-gel@5%Pt on -alumina sample calcined at 350oC which shows no further change when compared with the spectrum of the Figure S1B. This fact clearly suggests that the formation of Si-O-Al linkage from the dehydroxylation (gelation) reaction of the Si-OH and Al-OH has been readily occurred at ambient conditions.

Fig. S2 Optical spectra of Silica-gel@5%Pt and Silica-gel@5%(Ag0.67Pt0.33) powders

It is noted that our new results of the coated alloy composite clearly shows a plasmon peak at about 330 nm where coated pure Pt shows no absorption peak. The slight shift of the 330nm peak of the Ag0.67Pt0.33 alloy as compared with the 350 nm in the literature1 can be attributed to adsorbed nucleophile on the alloy particles such as OH- during our synthesis, which is known to increase on concentration of conduction electron in metal particle resulting in the blue shift1.