# Supplementary data

In situ co-crystallisation as a tool for low-temperature crystal engineering

Andrew D. Bond

S1. Melting point determination

Melting points were determined in situ by warming the single crystal after data collection. The temperature measured is the point at which the diffraction pattern is lost. Determination of the melting point in this manner is convenient since the entire experiment may be performed in situ on the diffractometer. All values were measured on the same instrument using the same N2 cryostream, so that the relative melting points (relevant to the discussion of the alternation effect) are as accurate as possible. The absolute values of the melting points are somewhat less accurate since the temperature measured at the nozzle of the gas stream is not the same as the temperature at the sample. To calibrate the temperature on an absolute scale, the melting points of heptanoic, octanoic, nonanoic and decanoic acid (in 0.2 mm capillaries) were measured by the same technique. These measurements clearly illustrate the melting point alternation in the pure n-alkyl carboxylic acids (confirming that the relative values are reliable), and provide calibration points across the entire temperature range of the melting points of 1–10. Comparison with literature values (Aldrich) suggest that a correction of ca. 10 K is appropriate across the entire range. The melting points given in the main text are the corrected values, quoted to 3 significant figures.

Calibration measurements:

|  | Measured at nozzle (K) | Literature Value (K) |  (K) |
| --- | --- | --- | --- |
| Heptanoic acid | 271 | 262 | -9 |
| Octanoic acid | 299 | 289 | -10 |
| Nonanoic acid | 293 | 282 | -11 |
| Decanoic acid | 316 | 305 | -11 |

m.p. / K

Measured

Literature

Heptanoic acid

Octanoic acid

Nonanoic acid

Decanoic acid

# Supplementary information

In situ co-crystallisation as a tool for low-temperature crystal engineering

Andrew D. Bond

Melting point measurements for 1–10:

|  | Measured at nozzle (K) | Corrected value (K) |
| --- | --- | --- |
| 1 |  |  |
| 2 | 278 | 268 |
| 3 | 262 | 252 |
| 4 | 270 | 260 |
| 5 | 270 | 260 |
| 6 | 282 | 272 |
| 7 | 292 | 282 |
| 8 | 293 | 283 |
| 9 | 305 | 295 |
| 10 | 310 | 300 |

Corrected melting points (K):

# Supplementary information

In situ co-crystallisation as a tool for low-temperature crystal engineering

Andrew D. Bond

S2. Variation of melting point and crystal density for 1-10

m.p. / K

Dc / g cm-3