Electronic Supplementary Information

Donor-substituted cyanoethynylethenes: powerful chromophores for opto-electronic applications

Nicolle N. P. Moonena, Robin Gista, Corinne Boudonb, Jean-Paul Gisselbrechtb, Paul Seilera, Tsuyoshi Kawaic, Atsushi Kishiokac, Maurice Grossb, Masahiro Iriec and François Diederich*,a

aLaboratorium für Organische Chemie, ETH-Hönggerberg, HCI, CH-8093 Zürich, Switzerland. Email: diederich@org.chem.ethz.ch

bLaboratoire d’Electrochimie et de Chimie Physique du Corps Solide, UMR 7512, C.N.R.S., Université Louis Pasteur, 4, rue Blaise Pascal, F-67000 Strasbourg, France

cDepartment of Chemistry and Biochemistry, Graduate School of Engineering, Kyushu University, Hakozaki 6-10-1, Higashiku, Fukuoka 812-8581, Japan

Electronic Supplementary Information

Fig. 1 Crystal packing of 5, showing the slipped parallel stacking of the phenyl rings.

Electronic Supplementary Information

Fig. 2 UV/Vis spectra of CEEs 4 and 5 and of TEEs 8 and 9 in CHCl3.

Electronic Supplementary Information

Fig. 3 Structure of the AF-50 standard.

Electronic Supplementary Information

Table 1. Cyclic voltammetry and rotating disk voltammetry data in CH2Cl2 (+0.1 M n-Bu4NPF6): potentials vs. Fc/Fc+. Working electrode: glassy carbon electrode; counter electrode: Pt; reference electrode: Ag/AgCl. Scan rate: 0.1 V s–1

|  | Cyclic Voltammetry |  |  | Rotating Disk Voltammetry |  |
| --- | --- | --- | --- | --- | --- |
|  | Eo/ Va | Ep /mV | Ep /mVb | E1/2 /V | Slope /mV |
| 1 | +0.56 -1.64 | 80 90 | -2.26 -2.37 | +0.59 (1 e-) -1.70 (1 e-) | 60 70 |
| 2 | +0.56 -1.64 | 75 75 | -2.25 -2.35 | +0.59 (1 e-) -1.67 (1 e-) -2.39 (2 e-) | 70 75 150 |
| 3 | +0.67 -1.24 | 125 125 |  | +0.67 (1 e-) -1.32 (1 e-) | 70 100 |
| 4 | -1.31 | 60 | +0.63 -2.02 -2.20 | +0.65 (2 e-) -1.35 (1 e-) -2.06 | 50 70 75 |
| 5 | +0.50 +0.58 -1.38 | 70 70 70 | -1.95 -2.05 -2.20 | c) -1.44 (1 e-) | 100 |
| 6 | +0.79 | 65 | -0.86 | +0.79 (1 e-) -0.85 (1 e-) | 60 60 |
| 7 | +0.69 -0.74 -0.92 | 120 60 70 | -2.25 | +0.70 (2 e-) -0.77 (1 e-) -0.95 (1 e-) -2.31 (2 e-) | c) 60 60 75 |
| a Eo = (Epc + Epa)/2, where Epc and Epa correspond to the cathodic and anodic peak potentials, respectively. b Ep = irreversible peak potential c Electrode inhibition during oxidation. No plateau limiting current could be observed. |  |  |  |  |  |